y

DATA SHEET

MULTILAYER CERAMIC CAPACITORS

CC Series

NP0

16V TO 100V

Product Specification – Jul 07, 2004 V.6 Supersedes Date of Mar. 12, 2004

|  |  |  |  |  |  | 2 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Surface Mount Multilayer Ceramic Capacitors | CC | SERIES | NP0, 16V to 100V | 10 |  |  |  |

SCOPE

This specification describes Yageo CC NP0 series chip capacitors.

ORDERING INFORMATION

Part number is identified by the series, size, tolerance, packing style, temperature coefficient, rated voltage and capacitance value.

CC   NPO   BN 

(1)	(2) (3)	(4)	(5)

(1) SIZE

0402 (1005)

0603 (1608)

0805 (2012)

1206 (3216)

1210 (3225)

1812 (4832)

(2) TOLERANCE

B = ±0.1pF

C = ±0.25pF

D = ±0.5pF

F = ±1%

G = ±2%

J = ±5%

(3) PACKING STYLE

R = 7” paper tape

K = 7” blister tape

P = 13” paper tape

F = 13” blister tape

C = Bulk case

(4) RATED VOLTAGE

7 = 16V

8 = 25V

9 = 50V

0 = 100V

(5) CAPACITANCE VALUE:

First two for significant figures and 3rd for number of zero

Letter “R” for decimal point

CONSTRUCTION

|  | terminations |  |
| --- | --- | --- |
|  | electrodes |  |
| Fig. 1 Surface mounted multilayer | MLB457 |  |
| ceramic capacitor construction | ceramic material |  |

DIMENSION

For dimensions see Table 1

T	W

| Fig. 2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Surface mounted multilayer ceramic |  |  |  |  |  |  |  | L 2 |  |  | L 4 |  |  |  | L 3 |  |  | MBB211 |  |  |
|  | capacitor dimension |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | L 1 |  |  |  |  |  |  |  |  |  |
| Table 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| TYPE |  | CC0402 | CC0603 | CC0805 |  |  |  |  |  | CC1206 |  |  |  | CC1210 |  |  |  |  |  | CC1812 |  |
| L1 (mm) |  | 1. 0±0.05 | 1.6±0.10 | 2.0±0.10 |  |  |  |  |  | 3.2±0.15 |  |  |  | 3.2±0.20 |  |  |  |  |  | 4.5±0.20 |  |
| W (mm) |  | 0.5±0.05 | 0.8±0.07 | 1.25±0.10 |  |  |  |  |  | 1.6±0.15 |  |  |  | 2.5±0.20 |  |  |  |  |  | 3.2±0.20 |  |
| T (mm) | min. | 0.45 | 0.73 | 0.50 |  |  |  |  |  | 0.50 |  |  |  | 0.50 |  |  |  |  |  | 0.50 |  |
|  | max. | 0.55 | 0.87 | 1.35 |  |  |  |  |  | 1.35 |  |  |  | 1.80 |  |  |  |  |  | 1.80 |  |
|  | min. | 0.15 | 0.20 | 0.25 |  |  |  |  |  | 0.25 |  |  |  | 0.25 |  |  |  |  |  | 0.25 |  |
| L2/L3 (mm) max. |  | 0.30 | 0.50 | 0.75 |  |  |  |  |  | 0.75 |  |  |  | 0.75 |  |  |  |  |  | 0.75 |  |
| L4 (mm) | min. | 0.40 | 0.60 | 0.55 |  |  |  |  |  | 1.40 |  |  |  | 1.40 |  |  |  |  |  | 2.20 |  |

www.yageo.com Jul 07, 2005 V.6

|  |  |  |  |  |  | 3 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Surface Mount Multilayer Ceramic Capacitors | CC | SERIES | NP0, 16V to 100V | 10 |  |  |  |

CAPACITANCE RANGE & THICKNESS FOR 16V & 25V

| Table 2 |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CAPACITANCE |  |  | 16V |  | 25V |  |  |  |  |  |  |
| (pF) |  |  | 0402 | 0603 | 0402 | 0603 | 0805 | 1206 | 1210 |  |  |
| 150 |  |  |  |  |  |  |  |  |  |  |  |
| 180 |  |  |  |  | 0.5±0.05 |  |  |  |  |  |  |
| 220 |  |  |  |  |  |  |  |  |  |  |  |
| 270 |  |  |  |  |  |  |  |  |  |  |  |
| 330 |  |  | 0.5±0.05 |  |  |  |  |  |  |  |  |
| 390 |  |  |  |  |  |  |  |  |  |  |  |
| 470 |  |  |  |  |  |  |  |  |  |  |  |
| 560 |  |  |  |  |  |  |  |  |  |  |  |
| 680 |  |  |  |  |  |  |  |  |  |  |  |
| 820 |  |  |  |  |  |  |  |  |  |  |  |
| 1,000 |  |  |  |  |  | 0.8±0.07 |  |  |  |  |  |
| 1,200 |  |  |  |  |  |  |  |  |  |  |  |
| 1,500 |  |  |  |  |  |  |  |  |  |  |  |
| 1,800 |  |  |  |  |  |  |  |  |  |  |  |
| 2,200 |  |  |  | 0.8±0.07 |  |  |  |  |  |  |  |
| 2,700 |  |  |  |  |  |  |  |  |  |  |  |
| 3,300 |  |  |  |  |  |  | 0.85±0.1 |  |  |  |  |
| 3,900 |  |  |  |  |  |  | 1.25±0.1 |  |  |  |  |
| 4,700 |  |  |  |  |  |  |  |  |  |  |  |
| 5,600 |  |  |  |  |  |  |  |  |  |  |  |
| 6,800 |  |  |  |  |  |  |  |  |  |  |  |
| 8,200 |  |  |  |  |  |  |  | 0.85±0.1 |  |  |  |
| 10,000 |  |  |  |  |  |  |  |  |  |  |  |
| 12,000 |  |  |  |  |  |  |  |  | 0.6±0.1 |  |  |
| 15,000 |  |  |  |  |  |  |  |  | 0.85±0.1 |  |  |
| 18,000 |  |  |  |  |  |  |  |  |  |  |  |
| 22,000 |  |  |  |  |  |  |  |  | 1.15±0.1 |  |  |

www.yageo.com Jul 07, 2005 V.6

|  |  |  |  |  |  | 4 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Surface Mount Multilayer Ceramic Capacitors | CC | SERIES | NP0, 16V to 100V | 10 |  |  |  |

CAPACITANCE RANGE & THICKNESS FOR 50V & 100V

| Table 3 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CAPACITANCE |  |  | 50V |  |  |  |  |  |  |  | 100V |  |  |  |  |  |  |  |  |  |
| (pF) |  |  | 0402 | 0603 |  | 0805 | 1206 |  | 1210 | 1812 | 0603 |  | 0805 |  |  | 1206 |  | 1210 | 1812 |  |
| 0.47 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 0.56 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 0.68 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 0.82 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 1.0 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 1.2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 1.5 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 1.8 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2.2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2.7 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 3.3 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 3.9 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 4.7 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 5.6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 6.8 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 8.2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  | 0.5±0.05 | 0.8±0.07 |  | 0.6±0.1 | 0.6±0.1 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 10 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 12 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 15 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 18 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 22 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 27 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 33 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 39 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  | 0.8±0.07 |  |  | 0.6±0.1 |  | 0.6±0.1 |  |  |  |  |
| 47 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 56 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 82 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 100 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 120 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 150 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

180

220

www.yageo.com Jul 07, 2005 V.6

|  |  |  |  |  |  | 5 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Surface Mount Multilayer Ceramic Capacitors | CC | SERIES | NP0, 16V to 100V | 10 |  |  |  |

CAPACITANCE RANGE & THICKNESS FOR 50V & 100V (CONT.)

| Table 4 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CAPACITANCE |  | 50V |  |  |  |  |  | 100V |  |  |  |  |  |  |  |
| (pF) |  | 0402 | 0603 | 0805 | 1206 | 1210 | 1812 | 0603 | 0805 |  | 1206 | 1210 | 1812 |  |  |
| 270 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 330 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 390 |  |  | 0.8±0.07 |  |  |  |  | 0.8±0.07 |  |  |  |  |  |  |  |
| 470 |  |  |  | 0.6±0.1 |  |  |  |  |  |  |  |  |  |  |  |
| 560 |  |  |  |  |  |  |  |  | 0.6±0.1 |  |  |  |  |  |  |
| 680 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 820 |  |  |  |  | 0.6±0.1 |  |  |  |  |  | 0.6±0.1 |  |  |  |  |
| 1,000 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 1,200 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 1,500 |  |  |  | 0.85±0.1 |  |  |  |  |  | 0.85±0.1 |  |  |  |  |  |
| 1,800 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2,200 |  |  |  | 1.25±0.1 |  | 0.6±0.1 |  |  | 1.25±0.1 |  |  |  |  |  |  |
| 2,700 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 3,300 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 3,900 |  |  |  |  | 0.85±0.1 |  |  |  |  |  | 0.85±0.1 |  |  |  |  |
| 4,700 |  |  |  |  |  |  | 0.6±0.1 |  |  |  |  |  |  |  |  |
| 5,600 |  |  |  |  | 1.15±0.1 |  |  |  |  |  | 1.15±0.1 |  |  |  |  |
| 6,800 |  |  |  |  |  | 0.85±0.1 |  |  |  |  |  |  |  |  |  |
| 8,200 |  |  |  |  |  |  |  |  |  |  |  | 0.85±0.1 |  |  |  |
| 10,000 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 12,000 |  |  |  |  |  |  | 0.85±0.1 |  |  |  |  |  | 0.85±0.1 |  |  |
| 15,000 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 18,000 |  |  |  |  |  |  | 1.15±0.1 |  |  |  |  |  | 1.15±0.1 |  |  |
| 22,000 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

www.yageo.com Jul 07, 2005 V.6

|  |  |  |  |  |  | 6 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Surface Mount Multilayer Ceramic Capacitors | CC | SERIES | NP0, 16V to 100V | 10 |  |  |  |

THICKNESS CLASSES AND PACKING QUANTITY

| Table 5 |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| THICKNESS |  | 8mm TAPE WIDTH / AMOUNT PER REEL |  |  |  | 12mm TAPE WIDTH / |  |  |  |  |  |  |
| CLASSIFICATION |  |  |  |  |  | AMOUNT PER REEL | AMOUNT PER BULK CASE |  |  |  |  |  |
| (mm) |  | Ø180mm, 7” |  | Ø330mm, 13” |  | Ø180mm, 7” Blister |  |  |  |  |  |  |
|  |  | Paper | Blister | Paper | Blister | 1812 | 0402 |  | 0603 | 0805 |  |  |
| 0.5±0.05 | 10,000 |  | --- | 50,000 | --- | --- | 50,000 | --- |  | --- |  |  |
| 0.6±0.1 | 4,000 |  | --- | 20,000 | --- | --- | --- | --- |  | 10,000 |  |  |
| 0.8±0.07 | 4,000 |  | --- | 15,000 | --- | --- | --- | 15,000 |  | --- |  |  |
| 0.85±0.1 | 4,000 |  | --- | 15,000 | --- | --- | --- | --- |  | 8,000 |  |  |
| 1.15±0.1 | --- |  | 3,000 | --- | 10,000 | --- | --- | --- |  | --- |  |  |
| 1.25±0.1 | --- |  | 3,000 | --- | 10,000 | --- | --- | --- |  | 5,000 |  |  |

ELECTRICAL CHARACTERISTICS

| Table 6 |  |  |  |
| --- | --- | --- | --- |
| CHARACTERISTICS | TEST CONDITIONS | REQUIREMENT |  |
| Operation temperature range | --- | –55°C to +125°C |  |
| Temperature characteristic/coefficient (TC) | With respect to 20°C within operation | NP0=16V, 0±60ppm/K |  |
|  | temperature range | NP0>16V, 0±30ppm/K |  |

With respect to 20°C

Capacitance tolerance                           C≤1000pF 1Vrms/1MHz C>1000pF 1Vrms/1KHz

C<5; ±0.1pF, ±0.25pF

C≥5; ±0.25pF, ±0.5pF

C≥10pF; ±2%, ±5%

|  | With respect to 20°C | C<10pF |  |
| --- | --- | --- | --- |
|  |  | D.F. ≤10(3/C+0.7) x10-4 |  |
| Dissipation factor (D.F.) | C≤1,000pF 1Vrms/1MHz |  |  |
|  |  | or 30x10-4 whichever is less |  |
|  | C>1,000pF 1Vrms/1KHz |  |  |
|  |  | C≥10pF, D.F. ≤10x10-4 |  |
| Insulation resistance (IR) | At Ur (rated voltage) for 1 minute | Rins >10GΩ or Rins x C≥500s |  |
|  | Ur >500V, at 500V(DC) for 1minute | whichever is less |  |
| Dielectric withstanding Voltage | At 2.5x Ur (for Ur ≤100V) | No breakdown |  |
|  | 1.5x Ur +100V (for Ur >100V) for 5sec |  |  |

www.yageo.com Jul 07, 2005 V.6

|  |  |  |  |  |  | 7 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Surface Mount Multilayer Ceramic Capacitors | CC | SERIES | NP0, 16V to 100V | 10 |  |  |  |

TAPING REEL

| Table 7 |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| TAPE WIDE | 8mm | 8mm | 12mm |  | T |  |
| ØA (mm) | 180 | 330 | 180 |  |  |  |
| ØB (mm) | 62±1.5 | 62±1.5 | 62±1.5 |  |  |  |
| ØD (mm) | 20.5 | 20.5 | 20.5 | D | CBA |  |
| ØC (mm) | 12.75±0.15/–0 | 12.75±0.15/–0 | 12.75±0.15/–0 |  |  |  |
| W (mm) | 8.4+1.5/–0 | 8.4+1.5/–0 | 12.4+2/–0 |  |  |  |
| Tmax (mm) | 14.4 | 14.4 | 18.4 |  | MSA284_b |  |
|  |  |  |  |  | W |  |
|  |  |  |  | Fig. 3 Reel dimension | For dimension see Table 7 |  |

PAPER TAPE SPECIFICATION

| Table 8 |  |  |  |  |  | For dimension see Table 8 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DIMENSION | 0402 | 0603 | 0805 | 1206 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | P0 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| A (mm) | 0.62±0.05 | 1.10±0.05 | 1.65±0.05 | 2.0±0.1 |  |  | T |  |  |  |  |  |  |  |  |  | D 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | P2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| B (mm) | 1.12±0.05 | 1.90±0.05 | 2.4±0.05 | 3.5±0.1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| W (mm) | 8.0±0.2 | 8.0±0.2 | 8.0±0.2 | 8.0±0.2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  | cover tape |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | F |  |  |  |  |  |  |  |  |  |  |  |
| E (mm) | 1.75±0.1 | 1.75±0.1 | 1.75±0.1 | 1.75±0.1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | W |  |  |  |  |
| F (mm) | 3.5±0.05 | 3.5±0.05 | 3.5±0.05 | 3.5±0.05 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | B |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | A |  |  |  |  |  |  |  |  | P1 |  |  |  |  |  |  |  |  |  |  |  |  |  | MBG251_a |  |  |  |  |  |  |
| P0 (mm) | 4±0.05 | 4±0.05 | 4±0.05 | 4±0.05 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| P1 (mm) | 2±0.05 | 4±0.1 | 4±0.1 | 4±0.1 |  | Fig. 4 |  |  |  |  |  | Paper tape dimension |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| P2 (mm) | 2±0.05 | 2±0.05 | 2±0.05 | 2±0.05 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ØD0 (mm) | 1.5+0.1 | 1.5+0.1 | 1.5+0.1/–0 | 1.5+0.1/–0 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| T (mm) | 0.6±0.05 | 0.95±0.05 | 0.95±0.05 | 0.95±0.05 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

BLISTER TAPE SPECIFICATION

| Table 9 |  |  |  |  | For dimension see Table 9 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| DIMENSION | 0805 | 1206 | 1210 | 1812 |  |  |  |
| A (mm) | 0.20 | 0.30 | 0.30 | 0.40 |  | P0 |  |
|  |  |  |  |  | D 0 | P2 |  |
| B (mm) | 0.20 | 0.30 | 0.30 | 0.40 |  | E |  |
| W (mm) | 8.1±0.2 | 8.1±0.2 | 8.1±0.2 | 12.0±0.2 | pe | F |  |
|  |  |  |  |  |  | W |  |
| E (mm) | 1.75±0.1 | 1.75±0.1 | 1.75±0.1 | 1.75±0.1 |  |  |  |
|  |  |  |  |  |  | B |  |
| F (mm) | 3.5±0.05 | 3.5±0.05 | 3.5±0.05 | 5.5±0.05 |  |  |  |
| P0 (mm) | 4±0.1 | 4±0.1 | 4±0.1 | 4±0.1 |  | MBG516_a |  |
|  |  |  |  |  | A | D 1 |  |
| P1 (mm) | 4±0.1 | 4±0.1 | 4±0.1 | 8±0.1 | T | P1 |  |
| P2 (mm) | 2±0.05 | 2±0.05 | 2±0.05 | 2±0.05 | direction of unreeling |  |  |
| ØD0 (mm) | 1.5+0.1/–0 | 1.5+0.1/–0 | 1.5+0.1/–0 | 1.5+0.1/–0 | Fig. 5 Leader/trailer tape dimension |  |  |
| Tmax (mm) | 3.5 | 3.5 | 3.5 | 3.5 |  |  |  |

www.yageo.com Jul 07, 2005 V.6

|  |  |  |  |  |  | 8 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Surface Mount Multilayer Ceramic Capacitors | CC | SERIES | NP0, 16V to 100V | 10 |  |  |  |

PACKING METHOD

LEADER/TRAILER TAPE SPECIFICATION

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | leader end |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | cover tape only |  |  |
| trailer end |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | empty compartments |  |  |  |  |  | 120 40 mm |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | with cover tape |  |  |  |  |  |  |  |

|  |  | trailer (max. 260 mm) |  |  |  | leader 400 mm |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  | MEA529 - 2 |  |  |
| Fig. 6 Leader and trailer tape dimension |  |  |  |  |  |  |  |  |  |

METHOD OF MOUNTING

For normal use the capacitors may be mounted on printed-circuit boards or ceramic substrates by applying wave soldering, reflow soldering (including vapor phase soldering) or conductive adhesive in accordance with CECC 00802 classification A.

Typical values (sold line)

Process limits (dotted lines)

| 300 |  | 10 s | MLA859 |  |
| --- | --- | --- | --- | --- |
| T |  |  |  |  |
| (¡C) | 260 ¡C |  |  |  |
| 250 | 245 ¡C |  |  |  |
|  | 215 ¡C | 10 s |  |  |
| 200 |  | 40 s |  |  |
|  | 180 ¡C |  |  |  |

150

130 ¡C

100

2 K/s

50

0

0	50 100 150 200 250 t (s)

Fig. 7	Recommended reflow soldering profile

Typical values (sold line)

Process limits (dotted lines)

The capacitors may be soldered twice in accordance with this method if desired

300

10 s

| T |  |  |  |  | MLA861 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| (¡C) |  |  |  |  |  |  |  |
| 250 | 235 ¡C to 260 ¡C |  | second wave |  |  |  |  |
| 200 | first wave |  | 5 K/s |  |  |  |  |
|  |  |  | 2 K/s |  |  |  |  |
| 150 | 200 K/s |  |  |  |  |  |  |
|  | 100 ¡C to 130 ¡C | forced |  |  |  |  |  |
| 100 |  |  |  |  |  |  |  |
|  |  | cooling |  |  |  |  |  |
| 50 |  | 2 K/s |  |  |  |  |  |
| 0 |  |  |  |  |  |  |  |
| 0 | 50 | 100 | 150 | 200 | t (s) | 250 |  |

Fig. 8	Recommended wave soldering profile.

www.yageo.com Jul 07, 2005 V.6

|  |  |  |  |  |  | 9 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Surface Mount Multilayer Ceramic Capacitors | CC | SERIES | NP0, 16V to 100V | 10 |  |  |  |

TEST AND REQUIREMENT

| Table 10 |  |  |  |  |
| --- | --- | --- | --- | --- |
| IEC384-10 | TEST ITEMS | CONDITIONS | REQUIREMENTS |  |
| 4.9 | Bending | Bending rate 1mm/s, jig. radius 340mm | l∆C/Cl ≤1% |  |
| 4.10 | Resistance to soldering heat | 260±5°C for 10±0.5s in static solder bath | l∆C/Cl within 0.5% or 0.5pF |  |
|  |  |  | whichever is greater |  |
| 4.11 | Solderability | 2355C for 20.5s in a static solder bath | The termination shall be well tinned |  |
| 4.12 | Rapid change of temperature | –55°C to +125°C, 5 cycles | l∆C/Cl within 1% or 1pF, whichever is |  |
|  |  |  | greater |  |
|  |  |  | l∆C/Cl within 2% or 1pF whichever is |  |
| 4.14 | Damp heat | At 40°C, 90 to 95% RH | greater |  |
|  |  | and Ur applied for 500 hours | D.F. ≤2xspecified value |  |
|  |  |  | IR≥2,500MΩ or RxC≥25s, whichever is less |  |
|  |  | At upper category temperature | l∆C/Cl within 2% or 1pF whichever is |  |
|  |  |  | greater |  |
| 4.15 | Endurance | 2x Ur applied (1.5x Ur for Ur >50V) |  |  |
|  |  |  | D.F. ≤2xspecified value |  |

for 1,000 hours

www.yageo.com Jul 07, 2005 V.6

|  |  |  |  |  | 10 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Surface Mount Multilayer Ceramic Capacitors | CC | SERIES | NP0, 16V to 100V |  | 10 |  |  |

REVISION HISTORY

| REVISION | DATE | CHANGE NOTIFICATION | DESCRIPTION |
| --- | --- | --- | --- |
| Version 06 | Jul 07, 2005 | - | - Thickness updated |
| Version 05 | Mar 12, 2004 | - | - Thickness and packing quantity amending |
| Version 04 | Aug. 13, 2003 | - | - Taping drawing amended |
| Version 03 | Dec. 03, 2002 | - | - New Yageo edition |
| Version 02 | Jul. 04, 2002 | - | - |
| Version 01 |  |  |  |
| Version 0 |  |  | - First issue of this specification |

www.yageo.com Jul 07, 2005 V.6